Title:

Structure-properties of polysaccharides with various branching schemes

Authors & affiliations:

Rolland-Sabaté A.1, Grimaud, F.2, Irague, R.2, Guilois S.1, Lourdin, D.1, Putaux J-L3, Potocki-Véronèse, G.2, Buléon, A.1 - UR1268 Biopolymères Interactions Assemblages, INRA, F-44300 Nantes, France - LISBP, Université de Toulouse, INSA-UPS-INP, 135 Avenue de Rangueil, F-31077 Toulouse - CERMAV, UPR CNRS 5301, ICMG IFR 2607, BP 53, F-38041 Grenoble cedex 9 * Corresponding author : Agnes.Sabate@nantes.inra.fr

Abstract: (Your abstract must use Normal style and must fit in this box. Your abstract should be no longer than 300 words. The box will ‘expand’ over 2 pages as you add text/diagrams into it.)

The macromolecular characteristics, thermal properties and film-forming ability of branched glucose-based biopolymers presenting different structures were studied: glycogens, amylopectins and -D-glucans synthesized in vitro by dextransucrase mutants (dextrans) (Irague et al., 2012). Molar mass and size distributions were determined using asymmetrical flow field flow fractionation (A4F) coupled with multi-angle laser light scattering. The calculated macromolecular conformation and shape in solution were discussed as a function of the branching degree studied by NMR. Dextrans and glycogens showed very broad size distribution whereas an antagonistic trend was observed for amylopectins. The molar mass ranged from 5.2*106 to 1.8*107 g.mol-1, 1.2*108 to 4.2*108 g.mol-1 and from 7.6*107 to 6.0*108 g.mol-1 for glycogens, amylopectins and dextrans, respectively (Rolland-Sabaté et al., 2011; Irague et al., 2012). The branching degree varied from 6 to 8%, 3 to 5% and 3 to 20% for glycogens, amylopectins and dextrans, respectively. Glycogens and amylopectins exhibited a spherical conformation in solution with a Rg/Rh ratio characteristic of dendritic and hyperbranched structures respectively, whereas the series of dextrans exhibited more extended conformations from hyperbranched to comb-like structures. Glycogens and amylopectins had glass transition temperature around 90 °C and 110 °C in average. Dextrans exhibited glass transition temperature between 30 °C and 86 °C and some of them had a good film-forming ability and interesting mechanical properties. As for synthetic polymers, glass transition temperature of these alpha-glucans was shown to depend on both the branching characteristics (type of glycosidic linkage, number, type and topology of branching) and the molar mass. The determination of these structure-properties relations is of considerable interest for the design of biopolymer-based materials for food or non-food applications. References: Irague, R., Rolland-Sabaté, A., Roncalli-Tarquis, L., Doublier, J-L., Moulis, C., Monsan, P., Magali Remaud-Siméon, M., Potocki-Véronèse, G., Buléon, A.. Structure and property engineering of -D-glucans synthesized by dextransucrase mutants. Biomacromolecules (2012), in Press. Rolland-Sabaté, A., Guilois, S., Jaillais, B., Colonna, P. Molecular size and mass distributions of native starches using complementary separation methods: Asymmetrical Flow Field Flow Fractionation (A4F) and Hydrodynamic and High Performance Size Exclusion Chromatography (HDC-HPSEC), Analytical and Bioanalytical Chemistry, 399 (4), 1493-1505 (2011).